## Slide 1: Self-generated electron glasses in frustrated organic crystals
Louk Rademaker
(Kavli Institute for Theoretical Physics, Santa Barbara)
Leiden University, 4 December 2014

## Slide 2: In collaboration with:
Vladimir Dobrosavljevic (FSU)
Samiyeh Mahmoudian (FSU)
Simone Fratini (Institut Neel, FR)
Arnaud Ralko (Institut Neel, FR)

## Slide 3: Solid States
Crystals…
Crystalline SiO2
Tm ~ 2000 K
Supercooled liquid SiO2
Tg ~ 1400 K

## Slide 4: Supercooling a liquid

## Slide 5: Supercool properties
Loss of ergodicity at glass transition
Typical dynamical timescale for probing the phase-space is given by Arrhenius Law:
Slow dynamics governed by transitions from one metastable state to another, barrier Δ
1903

## Slide 6: Electronic States
Gas: free Fermi gas
Liquid: Landau Fermi liquid
Solid: Wigner crystal, or charge-density-wave
Electron glass: Disorder!
- Anderson Localization
- Many Body Localization

## Slide 7: Disorder-free electron glass?
Ref: Kagawa et al., Nat. Phys. 9, 413 (2013)
  (and Sato et al, JPSJ 2014; Sato et al, PRB 2014)
Material: Clean θ-(BEDT-TTF)2RbZn(SCN)4

## Slide 8: Resistivity data
Electron solid:
Stripe order
Supercool
electron liquid!

## Slide 9: Dynamical timescale
Equilibration experiments
Noise spectroscopy
Arrhenius Law!

## Slide 10: Local Charge clusters
Conclusion: “Charge-cluster glass”
X-ray studies of electronic order
‘Local’ order: not long-range

## Slide 11: Let’s do theory
Starting point is spinless interacting electrons
Program:
  Classical ground state (Variational Monte Carlo)
  Quantum ground state (Exact Diagonalization)
  Slow glassy dynamics (Metropolis Monte Carlo)

## Slide 12: Short-range interactions
Degeneracy of ground states
  (residual entropy!)
Zigzag Stripes
Straight Stripes
Three sublattice structure

## Slide 13: Pinball liquid
Taking quantum effects into account
Hotta & Furukawa, PRB 2006
Non-Fermi liquid with coexistence of localized and itinerant electrons
Ref: Merino, Ralko, Fratini, PRL 2013

## Slide 14: Long-range interactions
Pinball liquid is not θ-RbZn ground state
Battle the frustration by more frustration:
Known to cause self-generated glassiness and to stabilize stripe order
  Ref: Schmalian & Wolynes, PRL 2001; Rademaker et al, PRE 2013

## Slide 15: Long-range interactions
Linear stripes are lowest in energy:
Energy differences extremely small
Yet: linear stripes are robust!

## Slide 16: Exact diagonalization

## Slide 17: Finite Temperature Monte Carlo
Metropolis: accept local move with probability
Infinite range interactions on finite lattice?Ewald summation:

## Slide 18: Stripe charge order
Spinodal temperature Ts = 0.04V
Below Ts local update MC becomes non-ergodic

## Slide 19: Relaxation Time
Autocorrelation function
If system equilibrates
Exponential tail of C(t) gives relaxation time

## Slide 20: Relaxation Time
Arrhenius law, Δ = 0.2V

## Slide 21: Aging & Memory
Below Ts aging scaling

## Slide 22: Density Correlations

## Slide 23: Conclusion
θ-RbZn is a self-generated glass (no disorder)
Due to frustration between long-range interaction and triangular lattice
Effective classical model explains:
  Arrhenius relaxation behavior
  Local charge clusters